Supporting Information

Acetate production from inorganic carbon (HCO3-) in photo-assisted biocathode microbial electrosynthesis systems using WO3/MoO3/g-C3N4 heterojunctions and Serratia marcescens species

Zhenghong Caia, Liping Huanga,*, Xie Quana, Zongbin Zhaob, Yong Shia, Gianluca Li Pumac,*

aKey Laboratory of Industrial Ecology and Environmental Engineering, Ministry of Education (MOE), School of Environmental Science and Technology, Dalian University of Technology, Dalian 116024, China

bState Key Lab of Fine Chemicals, Liaoning Key Lab for Energy Materials and Chemical Engineering, School of Chemical Engineering, Dalian University of Technology, Dalian 116024, China

cEnvironmental Nanocatalysis & Photoreaction Engineering, Department of Chemical Engineering, Loughborough University, Loughborough LE11 3TU, United Kingdom

Corresponding authors:

(Huang L.) lipinghuang@dlut.edu.cn

(G. Li Puma) g.lipuma@lboro.ac.uk

Pages: 17

Tables: 3

Figures: 11

S2 Materials and methods

S2.1 Preparation of WO3/MoO3, g-C3N4 and WO3/MoO3/g-C3N4

The synthesis of g-C3N4 was as described by Shi et al. [29]. Briefly, melamine (10 g) was directly annealed at 550 °C for 3 h with a heating rate of 3 °C/min in a muffle furnace. The obtained yellow g-C3N4 sample was grinded into powder for further use. The g-C3N4 photocathode was realized through an impregnation method: The designed amounts of as-prepared g-C3N4 powder (0.5 g, 1.0 g, 1.5 g, 2.0 g) were firstly dissolved in 1000 mL deionized water and ultrasonicated for 10 hours at room temperature. The solution was then centrifuged for 10 minutes at 5000 r/min to obtain the supernatant. The graphite felt (Sanye Co., Beijing, China) with either 2.0 cm × 2.0 cm × 0.25 cm or 2.0 cm × 2.0 cm × 0.5 cm, was immersed in the supernatant for 12 h, and stored in the refrigerator for another 12 h. The graphite felt was finally dried through a vacuum freeze dryer (LGJ-10, Songyuan Huaxing Co., Beijng). The amount of g-C3N4 loaded onto the graphite felt cathode was calculated from the difference between the initial and the residual amounts of g-C3N4 in solution.

WO3/MoO3 species were in-situ electrodeposited onto the g-C3N4/graphite felt cathode through an electrodeposition method using a mixture of Na2MoO4·2H2O and Na2WO4·2H2O (Tianjin Bodi Chemistry Co., Ltd., analytical pure) as previously described [30-31]. The amount of WO3/MoO3 loaded onto the cathode was estimated from the difference between the initial and the residual concentrations of WO3 and MoO3 in solution.

S2.2 Evaluation of the electrotrophic viability in the presence of the photocatalyst and under light irradiation conditions

Briefly, both the catholyte and the cathode electrode were totally sampled from the reactors at the end of each fed-batch operation. The electrode was peeled off by sonication at a low specific power of 9 J/mL (Bran-sonic CPXH Ultrasonifier) in the catholyte. The solution was then centrifuged and the electrotrophic pellets were re-suspended in a physiological saline solution. An appropriate amount of aqueous propidium iodide was added to the physiological saline solution to reach a concentration of 50 ug/mL. The cells were then cultured at 37 °C for 10-20 minutes in the dark. After rinsing (twice) and re-suspension in physiological saline solution, the electrotrophic cells were quantified using a FD FACSCanto flow cytometer (Bioscience).

References

- K.P. Nevin, T.L. Woodard, A.E. Franks, Z.M. Summers, D.R. Lovley, Microbial electrosynthesis: Feeding microbes electricity to convert carbon dioxide and water to multicarbon extracellular organic compounds, mBio. 1 (2010) e00103-10. https://doi.org/10.1128/mbio.00103-10

- K.P. Nevin, S.A. Hensley, A.E. Franks, Z.M. Summers, J. Ou, T.L. Woodard, O.L. Snoeyenbos-West, D.R. Lovley, Electrosynthesis of organic compounds from carbon dioxide is catalyzed by a diversity of acetogenic microorganisms, Appl. Environ. Microbiol. 77 (2011) 2882-2886. https://doi.org/10.1128/AEM.02642-10

[3] T. Zhang, H. Nie, T.S. Bain, H. Lu, M. Cui, O.L, Snoeyenbos-West, A.E. Frank, K.P. Nevin, T.P. Russell, D.R. Lovley, Improved cathode materials for microbial electrosynthesis, Energy Environ. Sci. 6 (2012) 217–224. https://doi.org/10.1039/c2ee23350a

[4] H. Nie, T. Zhang, M. Cui, H. Lu, D. Lovley, T. Russell, Improved cathode for high efficient microbial-catalyzed reduction in microbial electro-synthesis cells, Phys. Chem. Chem. Phys. 15 (2013) 14290-14294. https//doi.org/10.1039/c3cp52697f

[5] N. Aryala, A. Halderb, P. Tremblaya, Q. Chi, T. Zhang, Enhanced microbial electrosynthesis with three-dimensional graphene functionalized cathodes fabricated via solvothermal synthesis, Electrochim. Acta. 217 (2016) 117-122. https//doi.org/10.1016/j.electacta.2016.09.063

[6] N. Aryal, L. Wan, M.H. Overgaard, A.C. Stoot, Y. Chen, P.L. Tremblay, T. Zhang, Increased carbon dioxide reduction to acetate in a microbial electrosynthesis reactor with a reduced graphene oxide-coated copper foam composite cathode, Bioelectrochemistry 128 (2019) 83-93. https//doi.org/10.1016/j.bioelechem.2019.03.011

[7] M. Cui, H. Nie, T. Zhang, D. Lovley, T. Russell, Three-dimensional hierarchical metal oxide carbon electrode materials for highly efficient microbial electrosynthesis, Sustain. Energ. Fuels 1 (2017) 1171-1176. https//doi.org/10.1039/c7se00073a

[8] S. Han, H. Liu, C. Zhou, H.J. Ying, Growth of carbon nanotubes on grapheme as 3D biocathode for NAD+/NADH balance model and high-rate production in microbial electrochemical synthesis from CO2, J. Mater. Chem. A 7 (2019) 1115-1123. https//doi.org/10.1039/C8TA10465D

[9] S. Bajracharya, A. ter Heijne, X. Benetton, K. Vanbroekhoven, C. Buisman, D. Strik, D. Pant, Carbon dioxide reduction by mixed and pure cultures in microbial electrosynthesis using an assembly of graphite felt and stainless steel as a cathode, Bioresour. Technol. 195 (2015) 14-24. https//doi.org/10.1016/j.biortech.2015.05.081

[10] C. Marshall, D. Ross, E. Fichot, R. Norman, H. May, Long-term operation of microbial electrosynthesis systems improves acetate production by autotrophic microbiomes, Environ. Sci. Technol. 47 (2013) 6023-6029. https//doi.org/10.1021/es400341b

[11] Z. Zaybak, J. Pisciotta, J. Tokash, B. Logan, Enhanced start-up of anaerobic facultatively autotrophic biocathodes in bioelectrochemical systems, J. Biotechnol. 168 (2013) 478-485. https//doi.org/10.1016/j.jbiotec.2013.10.001

[12] L. Jourdin, S. Freguia, B. Donose, J. Chen, G. Wallace, J. Keller, V. Flexer, A novel carbon nanotube modified scaffold as an efficient biocathode material for improved microbial electrosynthesis, J. Mater. Chem. A 2 (2014) 13093-13102. https//doi.org/10.1039/c4ta03101f

[13] L. Jourdin, T. Grieger, J. Monetti, V. Flexer, S. Freguia, Y. Lu, J. Chen, M. Romano, G. Wallace, J. Keller, High acetic acid production rate obtained by microbial electrosynthesis from carbon dioxide, Environ. Sci. Technol. 49 (2015) 13566-13574. https//doi.org/10.1021/acs.est.5b03821

[14] S. Gildemyn, K. Verbeeck, R. Slabbinck, S. Andersen, A. Prevoteau, K. Rabaey, Integrated production, extraction, and concentration of acetic acid from CO2 through microbial electrosynthesis, Environ. Sci. Technol. Lett. 2 (2015) 325-328. https//doi.org/10.1021/acs.estlett.5b00212

[15] S. Patil, J. Arends, I. Vanwonterghem, J. Meerbergen, K. Guo, G. Tyson, K. Rabaey, Selective enrichment establishes a stable performing community for microbial electrosynthesis of acetate from CO2, Environ. Sci. Technol. 49 (2015) 8833-8843. https//doi.org/10.1021/es506149d

[16] L. Jourdin, S. Freguia, V. Flexer, J. Keller, Bringing high-rate, CO2-based microbial electrosynthesis closer to practical implementation through improved electrode design and operating conditions, Environ. Sci. Technol. 50 (2016) 1982-1989. https://doi.org/10.1021/acs.est.5b04431

[17] S. Bajracharya, R. Yuliasni, K. Vanbroekhoven, C. Buisman, D. Strik, D. Pant, Long-term operation of microbial electrosynthesis cell reducing CO2 to multi-carbon chemicals with a mixed culture avoiding methanogenesis, Bioelectrochemistry 113 (2017) 26-34. https://doi.org/10.1016/j.bioelechem.2016.09.001

[18] S. Bajracharya, K. Vanbroekhoven, C. Buisman, D. Strik, D. Pant, Bioelectrochemical conversion of CO2 to chemicals: CO2 as a next generation feedstock for electricity-driven bioproduction in batch and continuous modes. Faraday Discussions 202 (2017), 433-449. https://doi.org/10.1039/c7fd00050b

[19] T. Song, H. Zhang, H. Liu, D. Zhang, H. Wang, Y. Yang, H. Yuan, J. Xie, High efficiency microbial electrosynthesis of acetate from carbon dioxide by a self-assembled electroactive biofilm, Bioresour. Technol. 243 (2017) 573-582. https://doi.org/10.1016/j.biortech.2017.06.164

[20] T. Song, K. Fei, H. Zhang, H. Yuan, Y. Yang, P. Ouyang, J. Xie, High efficiency microbial electrosynthesis of acetate from carbon dioxide using a novel graphene-nickel foam as cathode, J. Chem. Technol. Biotechnol. 93 (2018) 457-466. https://doi.org/10.1002/jctb.5376

[21] L. Yu, Y. Yuan, J. Tang, S. Zhou, Thermophilic moorella thermoautotrophica-immobilized cathode enhanced microbial electrosynthesis of acetate and formate from CO2, Bioelectrochemistry. 117 (2017) 23-28. https://doi.org/10.1016/j.bioelechem.2017.05.001

[22] G. Mohanakrishna, K. Vanbroekhoven, D. Pant, Imperative role of applied potential and inorganic carbon source on acetate production through microbial electrosynthesis, J. CO2 Utilization. 15 (2016) 57-64. https://doi.org/10.1016/j.jcou.2016.03.003

[23] Y. Xiang, G. Liu, R. Zhang, Y. Lu, H. Luo, High-efficient acetate production from carbon dioxide using a bioanode microbial electrosynthesis system with bipolar membrane, Bioresour. Technol. 233 (2017) 227-235. https://doi.org/10.1016/j.biortech.2017.02.104

[24] C. Marshall, D. Ross, E. Fichot, R. Norman, H. May, Electro-synthesis of commodity chemicals by an autotrophic microbial community, Appl. Environ. Microbiol. 78 (2012) 8412-8420. https://doi.org/10.1128/AEM.02401-12

[25] E. Blanchet, F. Duquenne, Y. Rafrafi, L. Etcheverry, B. Erable, A. Bergel, Importance of the hydrogen route in up-scaling electrosynthesis for microbial CO2 reduction, Energy Environ. Sci. 8 (2015) 3731–3744. https://doi.org/10.1039/c5ee03088a

[26] G. Mohanakrishna, K. Vanbroekhoven, D. Pant, Impact of dissolved carbon dioxide concentration on process parameters during its conversion to acetate through microbial electrosynthesis, React. Chem. Eng. 3 (2018) 371-378. https://doi.org/10.1039/c7re00220c

[27] Z. Dong, H. Wang, S. Tian, Y. Yang, H. Yuan, Q. Huang, T. Song, J. Xie, Fluidized granular activated carbon electrode for efficient microbial electrosynthesis of acetate from carbon dioxide, Bioresour. Technol. 269 (2018) 203-209. https://doi.org/10.1016/j.biortech.2018.08.103

[28] S. Tian, H. Wang, Z. Dong, Y. Yang, H. Yuan, Q. Huang, T. Song, J. Xie, Mo2C-induced hydrogen production enhances microbial electrosynthesis of acetate from CO2 reduction, Biotechnol Biofuels 12 (2019) 71. https://doi.org/10.1186/s13068-019-1413-z

[29] A. Shi, H. Li, S. Yin, J. Zhang, Y. Wang, H2 Evolution over g-C3N4/CsxWO3 under NIR light, Appl. Catal. B-Environ 228 (2018) 75–86.

https://doi.org/10.1016/j.apcatb.2018.01.070

[30] Q. Wang, L. Huang, X. Quan, G. Li Puma, Sequential anaerobic and electro-Fenton processes mediated by W and Mo oxides for degradation/mineralization of azo dye methyl orange in photo assisted microbial fuel cells, Appl. Catal. B-Environ. 245 (2019) 672-680. https://doi.org/10.1016/j.apcatb.2019.01.026

[31] Q. Wang, Z. Cai, L. Huang, Y. Pan, X. Quan, G. Li Puma, Intensified degradation and mineralization of antibiotic metronidazole in photo-assisted microbial fuel cells with Mo-W catalytic cathodes under anaerobic or aerobic conditions in the presence of Fe(III). Chem. Eng. J. 376 (2019) 119566. https://doi.org/10.1016/j.cej.2018.07.168

Fig. S1 Comparison of CVs of the WO3/MoO3/g-C3N4 electrodes in the presence (A) or the absence (B) of Serratia marcescens using Pt or carbon rod as a counter electrode.

Fig. S2 Broad SEM observation (A) on the biotic WO3/MoO3/g-C3N4 electrodes. EDS determination on the sites occupied by WO3/MoO3/g-C3N4 (B) or S. marcescens (C).

Fig. S3 Acetate production (A), residual hydrogen (B) and photo-response curves (C) under different amounts of inoculated electrotroph (OD600) (WO3/MoO3/g-C3N4: 19.2 (w/w, %); loading amount: 1.43 mg/cm2; cathode thickness: 5.0 mm; inorganic carbon: 2.4 mM; cathode potential: ‒0.6 V; solution conductivity: 5.8 mS/cm).

Fig. S4 Effect of loading of WO3/MoO3/g-C3N4 on acetate production (A), residual hydrogen (B) and photo-response curves (C) (cathode thickness: 2.5 mm; inorganic carbon: 24 mM; cathode potential: ‒1.1 V; solution conductivity: 103 mS/cm).

Fig. S5 Effect of ratios of WO3/MoO3 and g-C3N4 on acetate production (A), residual hydrogen (B), photo-response curves (C), and photoluminescence (PL) spectra (D) (cathode thickness: 2.5 mm; inorganic carbon: 24 mM; cathode potential: ‒1.1 V; solution conductivity: 103 mS/cm).

Fig. S6 Comparison of inorganic carbon consumption in the presence or absence of irradiation light (operational time: 0.5 d).

Fig. S7 Flow cytometry analysis of live/dead electrotrophs on the cathode of WO3/MoO3/g-C3N4 (A), WO3/MoO3 (B), g-C3N4 (C) or graphite felt (D) in the presence of light, or W/Mo/g-C3N4 in the absence of light (E) upon propidium iodide staining. The control of electrotroph without propidium iodide staining (F) (WO3/MoO3/g-C3N4: 19.2 (w/w, %); loading amount: 1.43 mg/cm2).

Fig. S8 Equivalent circuits

Fig. S9 CV test of the abiotic cathodes with or without (control) g-C3N4 or/and WO3/MoO3 deposits in the presence or absence (control) of light irradiation.

Fig. S10 Comparison of absorbance peak of p-hydroxybenzoic acid in HPLC as a probe of hydroxyl radicals under various cathode electrodes (A), and the established standard curve (B).

Fig. S11 Comparison of XRD (A) and XPS (B) on the new biotic WO3/MoO3/g-C3N4 cathodes or after 5 cycles operation.

Table S1 Comparative overview of acetate production from inorganic carbon in pure or mixed cultures cathodes of MES in the absence of solar light.

| Cathode electrode | Separator | Potential (V vs. SHE) | Current density (A/m2) | pH | Conductivity (mS/cm) | Temperature (°C) | Substrate | Electrotroph | Acetate production rate (mM/d) | CEacetate (%) | Reference |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Graphite sticks | CEM | ‒0.4 | 0.2 | --- | --- | --- | CO2 | Sporomusa ovata | --- | 86 | [1] |
| Graphite sticks | CEM | ‒0.4 | 0.01 ~ 0.03 | --- | --- | 37 | CO2 | S. sphaeroides; S. silvacetica; Clostridium aceticum; C. ljungdahlii; Moorella thermnocetica | --- | 48 ~ 88 | [2] |
| Carbon cloth | CEM | ‒0.4 | 0.7 | --- | --- | 25 | CO2 | S. ovata | 0.14 | 76 | [3] |
| Carbon cloth + Ni |  |  | 3.0 |  |  |  |  |  | 0.64 | 80 |  |
| Carbon cloth + Au |  |  | 3.9 |  |  |  |  |  | 0.85 | 83 |  |
| Carbon cloth + Pd |  |  | 3.2 |  |  |  |  |  | 0.66 | 79 |  |
| Graphite + nickel-nanowire | PEM | ‒0.4 | 8.9 | 7.0 | --- | --- | CO2 | S. ovata | 1.13 | 82 | [4] |
| Graphite |  |  | 1.0 |  |  |  |  |  | 0.49 | --- |  |
| Graphite + nickel nanoparticle |  |  | 1.7 |  |  |  |  |  | 0.03 | 84 |  |
| Carbon felt + graphene | PEM | ‒0.7 | 2.5 | --- | --- | --- | CO2 | S. ovata | 2.08 | 87 | [5] |
| Carbon felt |  |  | 0.4 |  |  |  |  |  | 0.31 | 77 |  |
| Reduced graphene oxide + copper | PEM | ‒1.0 | 21.6 | --- | --- | 25 | CO2 | S. ovata | 3.53 | 70 | [6] |
| Carbon felt + iron oxide | PEM | ‒0.7 | --- | --- | --- | 25 | CO2 | S. ovata | 5.95 | 86 | [7] |
| Carbon felt |  |  |  |  |  |  |  |  | 1.25 | 73 |  |
| Grapheme + carbon nanotubes | CEM | ‒0.6 | 0.6 | --- | --- | --- | --- | C. ljungdahlii | 0.26 | 83 | [8] |
| Grapheme |  |  | 0.5 |  |  |  |  |  | 0.17 | 82 |  |
| Carbon nanotubes |  |  | 0.3 |  |  |  |  |  | 0.09 | 75 |  |
| Graphite felt | PEM | ‒0.7 | 1.0 | 7.0 | --- | 30 | HCO3- (4 g/L) | C. ljungdahlii | 6.67 | 53 | [9] |
| Graphite granules | PEM | ‒0.6 | --- | --- | --- | 25 | CO2 | Mixed culture | 17.3 | 69 | [10] |
| Carbon fiber | CEM | ‒0.4 | 0.03 | 7.3 | --- | 30 | CO2 | Mixed culture | 0.20 | 35 | [11] |
| Reticulated vitreous carbon + carbon nanotube | CEM | ‒0.9 | 37 | 7.0 | --- | 35 | HCO3- (0.5-2 g/L) | Mixed culture | 0.42 | 70 | [12] |
| Carbon nanotubes on reticulated vitreous carbon | CEM | ‒0.9 | 17.7 | 6.7 | --- | 35 | HCO3- (1-4 g/L) | Mixed culture | 1.08 | 100 | [13] |
| Carbon felt/stainless steel | AEM/CEM | ‒1.1 | 5 | 7.7 | --- | 21 | CO2 | Mixed culture | 3.4 | 70 | [14] |
| Carbon felt | --- | ‒1.26 | 5 | 7.6 | --- | 28 | CO2 | Mixed culture | 1.0 | 58 | [15] |
| Carbon nanotubes on reticulated vitreous carbon | PEM | ‒1.1 ~ ‒0.5 | 34.8 | 5.2 ~ 6.7 | --- | 35 | HCO3- (1-4 g/L) | Mixed culture | 1.08 | 98 | [16] |
| Carbon felt/graphite stick | PEM | ‒0.8 | 10 | 7.0 | --- | 30 | CO2 | Mixed culture | 6.67 | 53 | [17] |
| Carbon felt | CEM | 3.1a | --- | 7.0 | --- | 30 | CO2 | Mixed culture | 1.67-2.48 | 34 | [18] |
| Carbon felt + reduced graphene oxide | PEM | ‒0.9 | 4.9 | 7.0 | --- | 25 | CO2 | Mixed culture | 1.83 ~ 2.83 | 77 | [19] |
| Carbon felt |  |  | 3.2 |  |  |  |  |  |  | 70 |  |
| Grapheme + nickel foam | PEM | ‒0.9 | 11.2 | 7.0 | --- | 25 | CO2 | Mixed culture | 3.11 | 70 | [20] |
| Nickel foam |  |  | 5.6 |  |  |  |  |  | 1.70 | 65 |  |
| Carbon cloth + carbon nanoparticles | PEM | ‒0.4 | 1.0 | 7.0 | --- | 55 | CO2 | M. thermoautrophica | 0.61 | 57 | [21] |
| Carbon cloth |  |  | 0.04 |  |  |  |  |  | 0.02 | 65 |  |
| Graphite | PEM | ‒0.6 ~ ‒0.8 | 1.5 ~ 39 | 7.0 | --- | 30 | HCO3- (2.5 g/L) | Mixed culture | 1.58 ~ 1.70 | --- | [22] |
|  |  |  |  |  |  |  | CO2 |  | 1.82 ~ 1.90 | --- |  |
| Graphite plate | PEM | 1.4a | 0.4 | --- | --- | 30 | CO2 | Mixed culture | 1.39 | 66 | [23] |
| Graphite granules/rod | PEM | ‒0.6 | --- | --- | --- | 25 | CO2 | Mixed culture | 4.00 | 67 | [24] |
| Stainless steel plate | CEM | ‒0.7 | 1.5 ~ 2.0 | 7.1 | 103 | 30 | CO2 | S. ovata | 14.7 | 53 | [25] |
| VITO-CoRE® | PEM | ‒0.6 | 0.1 | 7.0 | --- | 22 | HCO3- | Mixed culture | 2.33 | 56 | [26] |
| Granular activated carbon | PEM | ‒0.8 | 4.1 | --- | --- | 25 | CO2 | Mixed culture | 2.33 | 65 | [27] |
| Activated carbon + Mo2C | PEM | ‒0.9 | 5.2 | 6.8 | --- | 25 | CO2 | Mixed culture | 3.17 | 64 | [28] |

a: applied voltage; PEM: proton exchange membrane; CEM: cation exchange membrane; AEM: anion exchange membrane

Table S2 System performance under conditions of various cathode thickness (CT), inorganic carbon (IC) concentrations, cathode potentials (CP), solution conductivities (SC) and initial pHs (WO3/MoO3/g-C3N4: 19.2 (w/w, %); loading amount: 1.43 mg/cm2; inoculum of electrotroph at an OD600 of 0.35).

| Condition | Acetate production (mM/d) | Residual H2 (m3/m3/d) | Acetate-H2 (m3/m3/d) | H2 production (m3/m3/d) | NaHCO3 consumed (mM/d) | Current (A/m2) | CEacetate (%) | EIS |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  |  | Rs | Rct | Rdif |
| NaHCO3: 2.4 mM; CP: ‒0.6 V; CT: 5 mm; pH 5.8; SC: 5.8 mS/cm | 0.83 ± 0.03 | 0.001 ± 0.000 | 0.08 ± 0.01 | 0.08 ± 0.01 | 3.88 ± 0.05 | 0.7 ± 0.1 | 71 ± 2 | 15 | 38 | 1580 |
| NaHCO3: 24 mM; CP: ‒0.6 V; CT: 5 mm; pH: 5.8; SC: 5.8 mS/cm | 1.80 ± 0.03 | 0.001 ± 0.000 | 0.18 ± 0.01 | 0.18 ± 0.01 | 6.62 ± 0.12 | 1.1 ± 0.1 | 91 ± 3 | 14 | 41 | 449 |
| NaHCO3: 24 mM; CP: ‒1.1 V; CT: 5 mm; pH: 5.8; SC: 5.8 mS/cm | 2.37 ± 0.07 | 0.004 ± 0.001 | 0.23 ± 0.02 | 0.24 ± 0.02 | 7.79 ± 0.19 | 1.6 ± 0.1 | 88 ± 3 | 13 | 45 | 211 |
| NaHCO3: 24 mM; CP: ‒1.1 V; CT: 2.5 mm; pH: 5.8; SC: 5.8 mS/cm | 2.60 ± 0.10 | 0.006 ± 0.001 | 0.26 ± 0.02 | 0.26 ± 0.02 | 8.17 ± 0.17 | 1.7 ± 0.1 | 90 ± 4 | 8 | 36 | 80 |
| NaHCO3: 24 mM; CP: ‒1.1 V; CT: 2.5 mm; pH: 5.0; SC: 5.8 mS/cm | 2.27 ± 0.07 | 0.058 ± 0.005 | 0.22 ± 0.02 | 0.28 ± 0.02 | 7.71 ± 0.14 | 2.0 ± 0.1 | 66 ± 2 | 9 | 49 | 46 |
| NaHCO3: 24 mM; CP: ‒1.1 V; CT: 2.5 mm; pH: 5.8; SC: 103 mS/cm | 3.10 ± 0.10 | 0.002 ± 0.000 | 0.31 ± 0.02 | 0.31 ± 0.02 | 9.14 ± 0.21 | 2.5 ± 0.1 | 73 ± 2 | 5 | 32 | 30 |

Table S3 EIS parameters obtained from Nyquist plots and CV data on the biotic or abiotic cathodes (over-potentials for acetate at biotic cathode and hydrogen at abiotic cathode).

| Condition |  |  | EIS |  |  |  | CV |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | Rs (Ω) | Rct (Ω) | Rdif (Ω) |  | Eonset (V) | Ep (V) | Ip (mA) | Over-potential (V) |
| biotic | WO3/MoO3/g-C3N4 |  | 5.1 | 32 | 30 |  | ‒0.31 | ‒0.56 | ‒0.42 | 0.08 |
|  | WO3/MoO3/g-C3N4, no light |  | 6.5 | 43 | 33 |  | ‒0.32 | ‒0.55 | ‒0.31 | 0.09 |
|  | WO3/MoO3 |  | 4.1 | 60 | 35 |  | ‒0.34 | ‒0.52 | ‒0.27 | 0.13 |
|  | g-C3N4 |  | 3.3 | 74 | 33 |  | ‒0.42 | ‒0.51 | ‒0.21 | 0.21 |
|  | Bare graphite felt |  | 3.1 | 100 | 36 |  | ‒0.46 | ‒0.50 | ‒0.18 | 0.25 |
| abiotic | WO3/MoO3/g-C3N4 |  | 3.9 | 59 | 21 |  | ‒0.46 | ‒1.20 | ‒1.12 | 0.12 |
|  | WO3/MoO3/g-C3N4, no light |  | 4.3 | 68 | 24 |  | ‒0.48 | ‒1.20 | ‒0.98 | 0.14 |
|  | WO3/MoO3 |  | 3.1 | 88 | 25 |  | ‒0.50 | ‒1.20 | ‒0.89 | 0.16 |
|  | g-C3N4 |  | 2.3 | 113 | 26 |  | ‒0.52 | ‒1.20 | ‒0.57 | 0.18 |
|  | Bare graphite felt |  | 1.9 | 127 | 30 |  | ‒0.54 | ‒1.20 | ‒0.46 | 0.20 |