## Slide 1: Investigation of the Preparation of Monodispersed Liposome Suspensions Using Microsieve Membranes
A. Laouini1, 2, C. Charcosset2, R. G. Holdich1, G.T. Vladisavljevic1
1Department of Chemical Engineering, Loughborough University, United Kingdom
2Laboratoire d’Automatique et de Génie des Procédés, Université Claude Bernard Lyon 1, France
Acknowledgement: Abdallah LAOUINI held a CMIRA Explora 2011 fellowship from “Région Rhône-Alpes”
Mechanical stirring
Microsieve membrane
Experimental set-up
Liposomes preparation using a stirred cell
The ethanolic phase (containing the required amounts of phospholipid and stabilizer) was permeated thorough the pores of the microsieve membrane into the aqueous phase, using a peristaltic pump. Then, the liposomal suspension was allowed to stand for 15 min under mechanical stirring and finally ethanol was removed by rotary evaporation.
What happens at the interface between the 2 phases?
When reproducing the process in a single pore (using a microfluidic channel device), microscopic observation showed: (A) Dripping mode: droplets were attached to the pore surface, however once detached we couldn’t see them suspended in the continuous phase since ethanol is miscible in water. (B) Jetting mode: when the flow rate was increased, jets ended in multi-concentric waves were observed. (C) Spontaneous liposomes formation occurred immediately when both phases were in contact and liposome aggregates were observed.
(B)
(C)
Optimisation of the process parameters and formulation factors
Phospholipids concentration = 20 mg/ml
Aqueous to organic phase volume ratio = 4.5
Agitation speed = 600 rpm
Transmembrane flux = 142 L/m²/h
Stabilizer: cholesterol 5 mg/ml
Both Lipoid E80 and POPC could be used:
(Lipoid E80)
(POPC)
Drug loading test
Vitamin E was successfully encapsulated within liposomes. The encapsulation efficiency was = 99.87% for a drug to lipid ratio of 25%. The final concentration was 1.15 mg of vitamin E per ml of liposomes suspension.
Background
Liposomes are spherical nanovesicles composed of one or several concentric phospholipidic bilayers with an internal aqueous phase
Due to their biocompatibility and biodegradability, they have been extensively studied as drug carriers for efficacy enhancement and toxicity reduction
Several techniques have been reported for liposomes preparation: thin film hydration, reversed phase evaporation, solvent injection...
So far, only polymeric hollow fibre and tubular glass membranes have been used in the preparation of liposomes
Aims of the study
Develop and optimise a novel strategy for the preparation of liposomes, based on dispersion of organic phase through microsieve membrane in a stirred cell. The use of microsieve membranes with uniformly sized pores and constant pore spacing allows a uniform dispersion of organic phase over the membrane surface, which makes easier to extrapolate the results for an industrial production.
Investigate the reproducibility of the process
Study the stability of the liposomal suspensions
Apply this new process to the encapsulation of vitamin E
Microscopic observation 200 µm
Photo of the membrane
The optimum experimental conditions were:
Storage stability study
Effect of the membrane pore size
When the membrane pore size decreased, the liposomes mean size decreased as well. A linear relationship was obtained which confirms the possibility of controlling the preparation characteristics by tuning the membrane parameters.
Conclusion
A new process was developed for liposomes preparation using microsieve membranes
This new technique led to the formation of narrow distributed liposomes
Vitamin E was successfully encapsulated with a high entrapment efficiency
The process was reproducible and the preparations showed very good stability
The use of microsieve membranes for liposomes preparation is simple, fast, reliable and present a potential for production at a large scale
(A)