Supporting Information

Synergistic induced charge transfer switch by oxygen vacancy and pyrrolic nitrogen in MnFe2O4/g-C3N4 heterojunctions for efficient transformation of bicarbonate to acetate in photo-assisted MES

Weifeng Konga, Liping Huanga,*, Xie Quana, Gianluca Li Pumab,*

a Key Laboratory of Industrial Ecology and Environmental Engineering, Ministry of Education (MOE), School of Environmental Science and Technology, Dalian University of Technology, Dalian 116024, China

b Environmental Nanocatalysis & Photoreaction Engineering, Department of Chemical Engineering, Loughborough University, Loughborough LE11 3TU, United Kingdom

Corresponding authors:

lipinghuang@dlut.edu.cn (L. Huang)

g.lipuma@lboro.ac.uk (G. Li-Puma)

Pages: 12

Tables: 3

Figures: 11

S2 Materials and methods

S2.1 Preparation of MnFe2O4/g-C3N4 photocathodes

The MnFe2O4/g-C3N4 photocathode was prepared by an impregnation method: different amounts of as-prepared MnFe2O4/g-C3N4 powder (0.5, 1.0, 1.5, 2.0 g) were firstly dispersed in 1 L deionized water with 10 h ultrasonication and then centrifuged at 5000 r/min for 10 min to obtain supernatants. The graphite felts (2.0 cm × 2.0 cm × 0.25 cm, Sanye Co., Beijing, China) were immersed in the above supernatants overnight and dried at 60 °C for 12 h. The amounts of catalysts loaded on the cathodes were calculated from the differences between the residual and the initial amounts of catalysts in solution. Finally, the cathodes were calcined at 300 °C with a heating rate of 2 °C/min for 2 h in a muffle furnace. All the control cathodes were prepared by the above method for subsequent experiments.

Fig. S1 Mott-Schottky plots of the MnFe₂O₄/g-C₃N₄ (A), MnFe₂O₄ (B) and g-C3N4 (C), XPS survey spectra (D) and N2 adsorption-desorption isotherms (E and F) of various photocatalysts.

Fig. S2 SEM images (A, C and E) and EDS spectra (B, D and F) on abiotic electrodes with urea-untreated photocatalysts of MnFe2O4/g-C3N4 (A and B), MnFe2O4 only (C and D), and g-C3N4 only (E and F), element mapping images of urea-treated MnFe₂O₄/g-C3N4 (G-K).

Fig. S3 Acetate production (A), residual hydrogen (B), CEacetate (C) and inorganic carbon consumption (D) for MnFe₂O₄/g-C3N4 with different amounts of urea treatment.

Fig. S4 Transient photocurrent responses (A), acetate production (B), CEacetate (C) and inorganic carbon consumption (D) for urea-treated MnFe₂O₄/g-C3N4 at different ratios.

Fig. S5 Acetate production (A), residual hydrogen (B), CEacetate (C) and inorganic carbon consumption (D) for urea-treated MnFe₂O₄/g-C3N4 at different loading amounts.

Fig. S6 Comparison of current density of different cathodes under various conditions (operational time: 0.5 d).

Fig. S7 Flow cytometry analysis of live/dead electrotroph for urea-treated MnFe₂O₄/g-C3N4 (A), g-C3N4 (D) and MnFe₂O₄ (E) or urea-untreated MnFe₂O₄/g-C3N4 (B) and bare graphite felt (F) in the presence of light, or urea-treated MnFe₂O₄/g-C3N4 in the absence of light (C) upon propidium iodide staining. The control of electrotroph without propidium iodide staining (G).

Rs: solution and electrode resistance;

Rct: charge transfer resistance;

Rdif: diffusion resistance;

CPE: constant phase elecment.

Fig. S8 Equivalent circuits

Fig. S9 Time course of acetate production (A), residual hydrogen (B), CEacetate (C), inorganic carbon consumption (D), current density (E) and Nyquist plots of EIS spectra (F) of the different cathodes.

Fig. S10 Residual hydrogen (A), accumulated photocatalysts leaching (B) and Nyquist plots of EIS spectra (C) of the different cathodes over 24 days operation with periodical addition of bicarbonate.

Fig. S11 SEM images (A, C and E) and EDS spectra (B, D and F) on urea-treated electrodes of MnFe₂O₄/g-C3N4 (A and B), MnFe₂O₄ (C and D) or g-C3N4 (E and F) with the S. marcescens at the end of a 24 d operation with periodical addition of bicarbonate.

Table S1 CV and DPV data and EIS parameters obtained from Nyquist plots of the biotic or abiotic cathodes

| Condition |  | EIS |  | CV |  | DPV |
| --- | --- | --- | --- | --- | --- | --- |
|  |  | Rs (Ω) | Rct (Ω) | Rdif (Ω) |  | Eonset-acetate (V) | Ep-acetate (V) | Ip-acetate (mA) |  | Ep-acetate (V) | Ip-acetate (mA) | Ep-cytochrome c (V) | Ip-cytochrome c (mA) |
| biotic | MnFe₂O₄/g-C₃N₄-urea |  | 3.5 | 29 | 25.7 |  | -0.31 | -0.59 | -2.77 |  | -0.50 | -2.33 | 0.029 | -0.64 |
|  | MnFe₂O₄/g-C₃N₄-urea-no light |  | 3.5 | 37 | 26.8 |  | -0.39 | -0.75 | -1.10 |  | -0.58 | -1.87 | 0.014 | -0.52 |
|  | MnFe₂O₄/g-C₃N₄-no urea |  | 3.6 | 45 | 27.1 |  | -0.33 | -0.60 | -1.27 |  | -0.51 | -1.79 | 0.026 | -0.50 |
|  | MnFe₂O₄-urea |  | 5.0 | 60 | 26.2 |  | -0.34 | -0.61 | -0.82 |  | -0.51 | -1.65 | 0.025 | -0.46 |
|  | MnFe₂O₄-no urea |  | 5.1 | 66 | 25.8 |  | -0.36 | -0.62 | -0.65 |  | -0.53 | -1.63 | 0.024 | -0.45 |
|  | g-C₃N₄-urea |  | 4.5 | 69 | 26.5 |  | -0.35 | -0.61 | -0.74 |  | -0.51 | -1.71 | 0.026 | -0.48 |
|  | g-C₃N₄-no urea |  | 4.7 | 75 | 27.2 |  | -0.36 | -0.62 | -0.66 |  | -0.52 | -1.69 | 0.024 | -0.43 |
|  | Bare graphite felt |  | 3.1 | 82 | 28.6 |  | -0.44 | -0.75 | -0.36 |  | -0.53 | -1.15 | 0.016 | -0.33 |
| abiotic | MnFe₂O₄/g-C₃N₄-urea |  | 2.9 | 55 | 26.8 |  | -0.43 | -1.40 | -2.47 |  | --- | --- | --- | --- |
|  | MnFe₂O₄-urea |  | 4.0 | 80 | 27.9 |  | -0.47 | -1.40 | -1.28 |  | --- | --- | --- | --- |
|  | g-C₃N₄-urea |  | 3.9 | 99 | 27.1 |  | -0.48 | -1.40 | -1.18 |  | --- | --- | --- | --- |
|  | Bare graphite felt |  | 2.5 | 125 | 30.5 |  | -0.59 | -1.40 | -0.39 |  | --- | --- | --- | --- |

Table S2 Comparison of EIS parameters for different cathodes obtained from Nyquist plots as a function of operational time

|  | Rs (Ω) | Rct (Ω) | Rdif (Ω) |
| --- | --- | --- | --- |
| MnFe₂O₄/g-C₃N₄-urea-0.25 d | 3.6 | 29 | 29 |
| MnFe₂O₄/g-C₃N₄-urea-0.50 d | 3.6 | 30 | 52 |
| MnFe₂O₄/g-C₃N₄-urea-0.75 d | 3.6 | 30 | 1074 |
| MnFe₂O₄/g-C₃N₄-urea-1.00 d | 3.7 | 31 | 1352 |
| MnFe₂O₄/g-C₃N₄-urea-1.25 d | 3.8 | 32 | 1672 |
| MnFe₂O₄-urea-1.25 d | 5.2 | 65 | 67 |
| g-C₃N₄-urea-1.25 d | 4.8 | 74 | 60 |
| Bare graphite felt-1.25 d | 3.4 | 88 | 49 |
| MnFe₂O₄/g-C₃N₄-no urea-1.25 d | 4.0 | 43 | 65 |

Table S3 Comparison of EIS parameters obtained from Nyquist plots of different cathodes with interval supplementary bicarbonate.

|  | Rs (Ω) | Rct (Ω) | Rdif (Ω) |
| --- | --- | --- | --- |
| MnFe₂O₄/g-C₃N₄-urea-0.5 d | 3.6 | 30 | 52 |
| MnFe₂O₄/g-C₃N₄-urea-8.0 d | 3.8 | 31 | 51 |
| MnFe₂O₄/g-C₃N₄-urea-16.0 d | 3.9 | 31 | 52 |
| MnFe₂O₄/g-C₃N₄-urea-24.0 d | 4.0 | 32 | 52 |
| MnFe₂O₄/g-C₃N₄-no urea-0.5 d | 3.7 | 47 | 46 |
| MnFe₂O₄/g-C₃N₄-no urea-8.0 d | 3.6 | 56 | 43 |
| MnFe₂O₄/g-C₃N₄-no urea-16.0 d | 3.4 | 62 | 41 |
| MnFe₂O₄/g-C₃N₄-no urea-24.0 d | 3.4 | 71 | 40 |
| MnFe₂O₄-urea-0.5 d | 5.1 | 62 | 43 |
| MnFe₂O₄-urea-8.0 d | 5.3 | 64 | 42 |
| MnFe₂O₄-urea-16.0 d | 5.5 | 65 | 43 |
| MnFe₂O₄-urea-24.0 d | 5.5 | 65 | 43 |
| g-C₃N₄-urea-0.5 d | 4.5 | 72 | 40 |
| g-C₃N₄-urea-8.0 d | 4.7 | 75 | 42 |
| g-C₃N₄-urea-16.0 d | 4.8 | 76 | 40 |
| g-C₃N₄-urea-24.0 d | 4.8 | 77 | 41 |
| Bare graphite felt-0.5 d | 3.1 | 85 | 37 |
| Bare graphite felt-8.0 d | 3.2 | 86 | 39 |
| Bare graphite felt-16.0 d | 3.3 | 87 | 37 |
| Bare graphite felt-24.0 d | 3.4 | 88 | 39 |