SUPPLEMENTARY INFORMATION

Hydrothermal Co-liquefaction of Biomass and Plastic Wastes into Biofuel: Study on Catalyst Property, Product Distribution and Synergistic Effects

Swathi Mukundan,a,b,* Jonathan L. Wagner,a Pratheep K. Annamalai,c Devika Sudha Ravindran,b Girish Kumar Krishnapillai,b and Jorge Beltraminid

a Loughborough University, UKRI National Interdisciplinary Centre for Circular Chemical Economy, Department of Chemical Engineering, Epinal way, Loughborough, Leicestershire, UK, LE11 3TU.

b Cochin University of Science and Technology, Department of Applied Chemistry, University Road, Kalamassery, Kochi– 682022, Kerala, India.

c The University of Queensland, Australian Institute for Bioengineering & Nanotechnology, St Lucia, QLD- 4072, Australia.

d Queensland University of Technology, Centre for Agriculture and the Bioeconomy, Brisbane, QLD– 4000, Australia.

*Corresponding author E–mail address– s.mukundan@lboro.ac.uk

Calculations

Yield of Bio-oil (Wt. %)=Mass of bio-oil gMass of feed g*100

Yield of Solids (Wt. %)=Mass of solid collected after reaction (g)Mass of feed (g)*100

Yield of Gas (Wt. %)=Mass of gas collected after reaction (g)Mass of feed (g)*100

Yield of aqueous phase %=100-yield of (bio-oil+solids+gas)

Deoxgenation %=Molar ratio ofOC in feed- Molar ratio ofOCin bio-oilMolar ratio ofOC in feed*100

Carbon recovery %=Mass of C in bio-oilMass of C in feed*100

HHV (MJ/Kg)=(0.363302*C)+(1.087033*H)-(0.100992*O)

Fig. S1a. SEM–EDAX of Mo/alumina catalyst

Fig. S1b. SEM–EDAX of Nb/alumina catalyst

Fig. S1c. SEM–EDAX of Ni/alumina catalyst

Fig. S1d. SEM–EDAX of W/alumina catalyst

Fig. S2. The yield % of bio-oil, aqueous, gas and solid products obtained from the hydrothermal co-liquefaction of Prosopis juliflora (PJ) and with the addition of polypropylene (PP) in different percentage (25 %, 33 %, 50 %, 67 %, 75 %) at temperature of (a) 340 ˚C, (b) 360 ˚C, (c) 380 ˚C, (d) 400 ˚C, (e) 420 ˚C, and (f) 440 ˚C for 60 min (non-catalytic reactions).

Fig. S3.   Comparison of the obtained bio-oil yield (%) and the calculated (anticipated) bio-oil yield (%) obtained with different PP addition to PJ (a) 25 %, (b) 33 %, (c) 50 %, (d) 67 %, and (e) 75 % at temperature of 340 ˚C, 360 ˚C, 380 ˚C, 400 ˚C, 420 ˚C, and 440 ˚C for 60 min (non-catalytic reactions).

Fig. S4. Comparison of the obtained yield of bio-oil with the calculated anticipated yield from the hydrothermal co-liquefaction of Prosopis juliflora (PJ) and with the addition of polypropylene (PP) in different PP percentage of (a) 25 %, (b) 33 %, (c) 50 %, (d) 67 %, (e) 75 % at 420 ˚C for 60 min in the presence of catalysts.

Fig. S5. Deconvoluted spectra of Nb 3d region of Nb/alumina catalyst

Fig. S6. % Selectivity of products in gas for the hydrothermal liquefaction of 1:3 (PP: PJ) with non-catalytic and Mo/alumina, Ni/alumina, Nb/alumina, and W/alumina catalysts (Catalyst: feed= 1: 50, Temperature= 420 °C, time= 60 min).