SUPPLEMENTARY MATERIAL

Electrospun PVA membranes reinforced with cellulose nanocrystals and thermally reduced graphene oxide: thermal, mechanical and UV-protection properties

P. Salazar-Bravoa, A. M. Torres-Huertab*, M. A. Domínguez-Crespob**, S. B. Brachetti-Sibajac, A.I. Licona-Aguilarc, A.E. Rodríguez-Salazard, H. Willcocke.

aInstituto Politécnico Nacional, CICATA-Altamira, km 14.5 Carretera Tampico-Puerto Industrial Altamira, C.P. 89600, Altamira, Tamaulipas, México

bInstituto Politécnico Nacional, UPIIH, km. 1+500, Carretera Pachuca-Actopan, C.P.42162, San Agustín Tlaxiaca, Hgo, México.

cTecnológico Nacional de México, IT de Ciudad Madero, D.E.P.I. Ave Primero de Mayo S.N. Col. Los Mangos. C.P. 89449 Cd. Madero, Tamps. México.

dInstituto Politécnico Nacional, CICATA Querétaro, Cerro Blanco 141, Col. Colinas del Cimatario, C.P. 76090, Santiago de Querétaro, Querétaro. México.

eDepartment of Materials, Loughborough University, Loughborough LE11 3TU, United Kingdom.

*E-mail corresponding authors: **atorresh@ipn.mx, mdominguezc@ipn.mx

| PVA (4 wt.%) |  |
| --- | --- |
| a) 3000x 1 µm | b) 1 µm 10000x |
| PVA (6 wt.%) |  |
| c) 3000x 1 µm | d) 3000x 1 µm |
| PVA (8 wt.%) |  |
| e) 10 µm 1000x | f) 1 µm 3000x |
| PVA (10 wt.%) |  |
| g) 100 µm 100x | h) 1 µm 3000x |

Figure S1. Morphological changes of PVA electrospun fibers in dependence of the concentration analyzing different zones and magnifications a-b) 4 wt.%, c-d) 6 wt.%, e-f) 8 wt.% and g-h) 10 wt.%.

PVA (8 wt.%):CNC (95:5)

10 µm 1000x a)

PVA (8 wt.%):CNC (90:10)

10 µm 1000x b)

PVA (8 wt.%):CNC (85:15)

10 µm 1000x c)

Figure S2. SEM images of the PVA (8 wt.%):CNC electrospun fibers using different ratio at different magnifications a) PVA:CNC (95:5), b) PVA:CNC (90:10) and c) PVA:CNC (85:15).

PVA (8 wt.%):CNC:TrGO (94.5:5.0.0:0.5)

a) 10 µm 5000x

PVA (8 wt.%):CNC:TrGO (89.5:10.0:0.5)

1 µm b) 8000x

PVA (8 wt.%): CNC:TrGO (84.5:15.0:0.5)

1 µm 10000x c)

Figure S3. SEM images of the final PVA:CNC:TrGO composite fibers at different magnifications a) 89.5:10.0:0.5, b) 89.5:10.0:0.5 and c) 84.5:15.0:0.5

Figure S4. Pore diameter histograms of the final PVA:CNC (a-c) and PVA:CNC:TrGO (d-f) composite membranes.

Figure S5. Reflectance diffuse analysis of the electrospun films a) before and b) after adding TrGO powders using different compositions and its comparison with PVA fibers.