# Supplementary materials

# An iron ore-based catalyst for producing hydrogen and metallurgical carbon via catalytic methane pyrolysis for decarbonization of the steel industry

Mickella Dawkins a1, David Saal b, José F. Marco c, James C. Reynolds a, Sandra E. Dann a

a Department of Chemistry, Loughborough University, Epinal Way, Loughborough, LE11 3TU

b School of Business and Economics, Loughborough University, Epinal Way, Loughborough, LE11 3TU

c Instituto de Química Física Rocasolano, CSIC, 28006 Madrid, Spain

1  m.dawkins2@lboro.ac.uk

XRD analysis

A Bruker D8 Discover in transmission geometry with monochromated cobalt Kα1 radiation and a position sensitive detector was used to obtain XRD patterns. The cobalt source is monochromated with Kα = 1.789Å, operating at 35 kV and 40 mA. The data sets were acquired in continuous scanning mode over the 2θ range 20° – 80°, using a step size of 0.00750404° per second. The raw data was peak matched using EVA software and PDF-1997 database.

GC analysis

The exhaust gases were collected in foil, gas bags every 30 minutes for 5 hours. The gases were then analysed on an Agilent 8860 GC system equipped with a packed column (Agilent ShinCarbon ST) and a Thermal Conductivity Detector (TCD). Argon was the carrier gas, and the oven temperature was maintained at 150 °C for each analysis. The Clarity version 8.5 software was used to develop and control methods, run single or multiple samples, and view and modify run results. The hydrogen and methane concentrations were obtained using a calibration curve, that was made beforehand with known concentrations of hydrogen and methane.

FT-IR analysis

Figure S1. FT-IR spectrum of the unmilled iron ore

Raman analysis – iron oxide standards

- (ii)

(iii)    						(iv)

Figure S2. Raman spectra of four iron oxide standards: (i) FeO, (ii) Fe3O4, (iii) γ-Fe2O3, (iv) α-Fe2O3

SEM images – iron ore

(i)    				(ii)    				(iii)

(iv)     				(v)   				(vi)

Figure S3. SEM images (i) – (vi) showing changes in the morphology of the iron ore at milling times of 0, 60, 120, 180, 240 and 300 minutes respectively.

XRD analysis – iron ore

Figure S4. XRD patterns showing changes in the crystallinity of the iron ore at milling times of 0, 60, 120, 180, 240 and 300 minutes

Raman analysis – milled iron ore

Figure S5. Raman spectra showing changes in the iron oxide phases of the iron ore at milling times of 60, 120, 180, 240 and 300 minutes.

SEM images – carbonaceous material

(i)    						(ii)

(iii)    						(iv)

Figure S6. SEM images of the carbonaceous material formed during methane pyrolysis

XRD analysis – transmission medium

Figure 7. XRD pattern of the transmission medium

SEM-EDS – used catalyst

Figure S8. SEM-EDS elemental analysis of used catalyst